Press Release

# LATI: Broad range of specialist metal substitution products

Polymers replace brass fittings for sanitary, heating and plumbing applications

Wiesbaden, March 2008 – Italian compounding specialist LATI Industria Termoplastici SpA, Vedano Olona, expanded its portfolio of metal substitution products with new grades for its LATAMID, LATIGLOSS, LARAMID and LARTON ranges. Due to their excellent mechanical properties they are suitable for use in sanitary, heating and plumbing applications instead of brass and other metals that have previously been used. The good processibility of the polymers means that such components can be manufactured in a single injection moulding process, which leads to significant manufacturing cost reductions. Further potential for cost savings can be achieved by integrating functional components at the injection moulding stage, removing the need for downstream assembly steps. During the development of the new grades the company worked closely with a number of national and international manufacturers from the sanitary, heating and plumbing sectors.

LATAMID and LATIGLOSS polyamide (PA) 66 grades can contain up to 60% by weight glass fibre and are very cost effective. They have comparable mechanical strength to aluminium and at 220 MPa approximately the same tensile stress at break as metals. In comparison these polymers have better chemical resistance, toughness and notched impact strength. The compounds in the LATIGLOSS range also have a very good surface finish despite the high glass fibre loadings. On top of this various custom and metal effect colour matches can be produced. Typical applications for LATAMID and LATIGLOSS are pneumatic valves and pump casings as well as control elements.

LARAMID compounds are based on partly aromatic polyamides (Polyphthalamides=PPA) that are very strong, stiff and creep resistant and have excellent dimensional stability. Due to their good chemical resistance, low water absorption and heat deflection temperature they are suitable for humid and aggressive environments as well as high temperatures. Typical applications for LARAMID are pump casings for refrigeration units as well as covers for hydraulic pumps.

The LARTON range is comprised of compounds based on polyphenylene sulfide (PPS). They are available with a glass fibre content of up to 40% by weight and are characterized by their good dimensional stability even at high temperatures, excellent chemical resistance and high levels of creep and fatigue resistance. They are used for example for flow rate valves.

The LATI portfolio contains a large number of engineering and high performance polymers that are suitable for metal substitution in a variety of applications. Due to the industrial expansion in the emerging markets of the Far East the demand for metal is constantly growing. As a result of this steel, aluminium, copper and its alloys are in short supply and increasing in price. Engineers in many industries are therefore looking for opportunities to replace metals with polymers.

LATI Industria Termoplastici S.p.A. is one of the leading European manufacturers of engineering polymers. The company has more than 60 years experience in processing polymers and an excellent reputation with customers and partners for quality and service. Their product portfolio comprises 2,500 individually optimised compounds that are sold worldwide. Specialities include high performance polymers, self-extinguishing as well as reinforced and filled compounds for the electrical and electronics sectors, general industrial use and transportation systems. The company has around 300 employees and in 2006 had a turnover of 120 million Euros.

XXX

Further information:

Andreas Gertner,  LATI Industria Termoplastici Deutschland GmbH
Otto-von-Guericke-Ring 7,  D-65205 Wiesbaden 
Tel.:  +49 (0)61 22/90 82-15,  Fax:  +49 (0)61 22/90 82-22
E-Mail:  agertner@de.lati.com
Internet:  http://www.lati.com

Editorial contact and voucher copies:

Barbara Welsch,  KONSENS Public Relations GmbH & Co. KG,
Hans-Kudlich-Straße 25,  D-64823 Groß-Umstadt
Tel.:  +49 (0)60 78/93 63-0,  Fax:  +49 (0)60 78/93 63-20
E-Mail:  mail@konsens.de

Caption:

Italian compounding specialist LATI Industria Termoplastici SpA, Vedano Olona, expanded is portfolio of metal substitution products with new grades for its LATAMID, LATIGLOSS, LARAMID and LARTON ranges. They are particularly suitable for sanitary, heating and plumbing applications.

Photo: LATI Deutschland, Wiesbaden